Leaching of Vanadium from Slags

Andrea Miškufová1,a, Tomáš Havlik1,b, Jana Pirošková1,c, Pavol Liptai1,d, Patrik Kuruc1,e, Róberta Slezáková1,f

1Technical university of Košice, Faculty of Materials, Metallurgy and Recycling, Institute of Recycling Technologies, Letná 9, 042 00 Košice, Slovakia

a*andrea.miskufova@tuke.sk, btomas.havlik@tuke.sk, cjana.piroskova@tuke.sk, dpavol.liptai@tuke.sk, epatrik.kuruc@tuke.sk, froberta.slezakova@tuke.sk

Keywords: vanadium, leaching, ozone, EAF slag, stainless steel slag, ferrochromium slag

Abstract.

The paper describes vanadium leaching from steelmaking and ferrochromium slags in alkaline media. The content of vanadium in mentioned slags is relatively low (1 - 6 %), but its effective recovery as a critical raw material for EU is highly demanding. In the experimental part of this work the slags from EAF, stainless steel and FeCr production with vanadium content up to 0.07 % have been used. The leachability of vanadium from three different type of slags in alkaline solutions (NaOH, KOH, Na2CO3) under oxidizing (O3) and non-oxidizing conditions at room temperature was tested. The results showed that vanadium is slightly leached from slags in NaOH and KOH (up to ~ 3 %). The highest leaching efficiency ~ 14 %  for vanadium was achieved with EAF slag after one hour od leaching using ozone. The most suitable leaching media appeared 2 M Na2CO3 with O3 flow rate 8 g O3.h-1. This work was realized with the support of Horizon 2020 project (CHROMIC) under Grant Agreement No. 730 471.