Overview of technical and technological possibilities of recycling waste laminated glass

Miloš Matúša,*, Ľubomír Šooša, Marcela Pokusováa

a Slovak University of Technology in Bratislava, Faculty of Mechanical Engineering, Institute of Manufacturing Systems, Environmental Technology and Quality Management, Námestie slobody 17, 81231 – Bratislava, Slovakia

*milos.matus@stuba.sk

Abstract

Composite materials bring new possibilities and great advantages for design and construction. The problem arises when they become waste. In order to reduce the environmental burden, it is necessary to design and apply a method of their effective recycling. The study deals with the overview of problems with recycling of windshields and laminated glass from buildings. The wide analyse is based on the production process of this laminated glass, material and chemical composition, and the possibility of using recycled materials. But the fundamental problem is to delaminate these kind of glasses or separated the glass and the polyvinyl butyral interlayer. For next recycling process of glass and PVB is necessary to get very clean these materials.  The paper describes technical solutions for treatment this kind of waste and offer verified procedures for delamination process.

Keywords: laminated glass, windshields, windshields delamination, polyvinyl butyral, glass delamination, glass recycling, PVB layer recycling

Acknowledgements

The paper is a part of the research done within the project UNIVNET - University and industrial research-educational platform of the recycling society. The authors would like to thank the Ministry of Education, Science, Research and Sport of the Slovak Republic.